Demountable acoustic ceiling

Content

Demountable acoustic gypsum ceiling in recessed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Unity 3_600 x 600 x 12.5_E+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm
	Weight: 9.20-9.90 kg/m²

Edge: E+, recessed T-grid system (8 mm recess).
Perforation: Square 3.5x3.5mm holes, c/c 8.33mm, Perforation to edge.

Perforation percent: 17.2 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 69.2% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

200mm suspension without mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.50 | 0.80 | 0.85 | 0.75 | 0.75 | 0.80 | 0.80 | 0.80 |

200mm suspension with 45mm mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.60 | 0.90 | 0.90 | 0.85 | 0.85 | 0.85 | 0.90 | 0.90 |

Main runner
Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Cross-tees
	Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Wall connection
	Type: < L-profile or Shadow line trim>
	Material: 0.5mm galvanized steel
	Colour: White

Dimension: < 24x20mm or 15x15x8x25mm >

Suspension
	Type: Adjustable hanger

Dimension: < xxx - xxx mm >

Installation

- Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 120mm)

- Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 400 mm.

- Distance between hangers ≤ 1200 mm.

- Distance from wall to first load-bearing (main runner) section ≤ 600 mm.

- Distance between load-bearing (main runner) sections ≤ 1200 mm.

- Subdivision made with cross-tees length 1200 and 600 mm.

- Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.

Demountable acoustic ceiling

Content

Demountable acoustic gypsum ceiling in recessed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Unity 4_600 x 600 x 12.5_E+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm
	Weight: 9.20-9.90 kg/m²

Edge: E+, recessed T-grid system (8 mm recess).
Perforation: Round 4mm holes, c/c 10mm, Perforation to edge.

Perforation percent: 12.2 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 72.5% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

200mm suspension without mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.45 | 0.75 | 0.80 | 0.70 | 0.65 | 0.60 | 0.70 | 0.75 |

200mm suspension with 45mm mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.55 | 0.80 | 0.80 | 0.75 | 0.75 | 0.65 | 0.75 | 0.80 |

Main runner
Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Cross-tees
	Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Wall connection
	Type: < L-profile or Shadow line trim>
	Material: 0.5mm galvanized steel
	Colour: White

Dimension: < 24x20mm or 15x15x8x25mm >

Suspension
	Type: Adjustable hanger

Dimension: < xxx - xxx mm >

Installation

- Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 120mm)

- Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 400 mm.

- Distance between hangers ≤ 1200 mm.

- Distance from wall to first load-bearing (main runner) section ≤ 600 mm.

- Distance between load-bearing (main runner) sections ≤ 1200 mm.

- Subdivision made with cross-tees length 1200 and 600 mm.

- Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.

Demountable acoustic ceiling

Content

Demountable acoustic gypsum ceiling in recessed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Unity 8|15|20_600 x 600 x 12.5_E+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm
	Weight: 9.20-9.90 kg/m²

Edge: E+, recessed T-grid system (8 mm recess).
Perforation: Random round 5|8|15|20mm holes, Perforation to edge.

Perforation percent: 10.8 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 72.2% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

200mm suspension without mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.40 | 0.55 | 0.60 | 0.60 | 0.50 | 0.50 | 0.60 | 0.55 |

200mm suspension with 45mm mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.45 | 0.60 | 0.55 | 0.60 | 0.55 | 0.60 | 0.60 | 0.55 |

Main runner
Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Cross-tees
	Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Wall connection
	Type: < L-profile or Shadow line trim>
	Material: 0.5mm galvanized steel
	Colour: White

Dimension: < 24x20mm or 15x15x8x25mm >

Suspension
	Type: Adjustable hanger

Dimension: < xxx - xxx mm >

Installation

- Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 120mm)

- Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 400 mm.

- Distance between hangers ≤ 1200 mm.

- Distance from wall to first load-bearing (main runner) section ≤ 600 mm.

- Distance between load-bearing (main runner) sections ≤ 1200 mm.

- Subdivision made with cross-tees length 1200 and 600 mm.

- Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.

Demountable acoustic ceiling

Content

Demountable acoustic gypsum ceiling in recessed T-grid system.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Unity 9_600 x 600 x 12.5_E+

Material: Perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm
	Weight: 9.20-9.90 kg/m²

Edge: E+, recessed T-grid system (8 mm recess).
Perforation: Square 9x9mm holes, c/c 20mm, Perforation to edge.

Perforation percent: 18.9 %

Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 71.6% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

200mm suspension without mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.45 | 0.75 | 0.85 | 0.75 | 0.75 | 0.65 | 0.75 | 0.80 |

200mm suspension with 45mm mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.55 | 0.85 | 0.85 | 0.80 | 0.85 | 0.80 | 0.85 | 0.85 |

Main runner
Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Cross-tees
	Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Wall connection
	Type: < L-profile or Shadow line trim>
	Material: 0.5mm galvanized steel
	Colour: White

Dimension: < 24x20mm or 15x15x8x25mm >

Suspension
	Type: Adjustable hanger

Dimension: < xxx - xxx mm >

Installation

- Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 120mm)

- Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 400 mm.

- Distance between hangers ≤ 1200 mm.

- Distance from wall to first load-bearing (main runner) section ≤ 600 mm.

- Distance between load-bearing (main runner) sections ≤ 1200 mm.

- Subdivision made with cross-tees length 1200 and 600 mm.

- Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.

Demountable acoustic ceiling

Content

Demountable acoustic gypsum ceiling in recessed T-grid system.
100% recyclable product.

Products and materials

Regula_600 x 600 x 12.5_E+

Material: Non-perforated plasterboard

Board Type: Ceiling tile

Dimensions: 600x600x12.5mm
	Weight: 9.20-9.90 kg/m²

Edge: E+, recessed T-grid system (8 mm recess).
Surface: Water-based acrylic paint

Colour: White NCS 0701 Y24R, (RAL 9003); gloss 5
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Light reflection: 82.6% in accordance with DIN 5036
Indoor climate: Degasification 10 days
Particle emission: Low

Acoustics

All suspension without mineral wool

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.40 | 0.20 | 0.10 | 0.05 | 0.05 | 0.05 | 0.10 | 0.05 |

Main runner
Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Cross-tees
	Type: T-profile

Material: 0.4mm galvanized steel
Colour: White

Dimensions: Width 15mm | Height 38mm

Wall connection
	Type: < L-profile or Shadow line trim>
	Material: 0.5mm galvanized steel
	Colour: White

Dimension: < 24x20mm or 15x15x8x25mm >

Suspension
	Type: Adjustable hanger

Dimension: < xxx - xxx mm >

Installation

- Screw spacing for attachment of wall connections max. 300mm c/c and in relation to the required ceiling height < xxx mm > (min. 120mm)

- Distance from wall to first hanger in direction of load-bearing (main runner) section ≤ 400 mm.

- Distance between hangers ≤ 1200 mm.

- Distance from wall to first load-bearing (main runner) section ≤ 600 mm.

- Distance between load-bearing (main runner) sections ≤ 1200 mm.

- Subdivision made with cross-tees length 1200 and 600 mm.

- Units of up to 3.0kg can be integrated directly into the ceiling tiles. 
In the case of heavier units, the unit must be installed independently without any load on the ceiling tile. 
For loads above 3kg/m², additional hangers must be used.