Acoustical deck and wall mount panels

Content

Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Micro_<900x2700> or < 1200x2400 > x 12.5_B1

Material: Perforated plasterboard

Board Type: Gypsum panel

Dimensions: <900x2700x12.5mm> or <1200x2400x12.5mm>
	Weight: 9.20-9.90 kg/m²

Edge: B1
Perforation: Square 3x3mm holes, c/c 8.33mm in patterns

Perforation percent: 7.1 - 9.8%

Surface: Unpainted cardboard

Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

65mm suspension with 50mm mineral wool (M1F)

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.40 | 0.60 | 0.65 | 0.65 | 0.60 | 0.55 | 0.65 | 0.65 |

Installation

- c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.

- Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations.

- Mount the furring crosswise the primary construction at a max c/c on 300mm.

- Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide.

- Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.

- When filler is completely dry then sand with a fine sandpaper.

- Use a fine short-haired mohair roller to apply paint.

Acoustical deck and wall mount panels

Content

Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Globe_<900x2700> or < 1200x2400 > x 12.5_B1
Material: Perforated plasterboard

Board Type: Gypsum panel

Dimensions: <900x2700x12.5mm> or <1200x2400x12.5mm>
	Weight: 9.20-9.90 kg/m²

Edge: B1
Perforation: Round 6mm holes, c/c 15mm in patterns

Perforation percent: 5.3 - 9.8%

Surface: Unpainted cardboard

Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

65mm suspension with 50mm mineral wool (G1F)

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.35 | 0.70 | 0.80 | 0.75 | 0.60 | 0.50 | 0.65 | 0.70 |

Installation

- c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.

- Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations.

- Mount the furring crosswise the primary construction at a max c/c on 300mm.

- Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide.

- Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.

- When filler is completely dry then sand with a fine sandpaper.

- Use a fine short-haired mohair roller to apply paint.

Acoustical deck and wall mount panels

Content

Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Quadril_<900x2700> or < 1200x2400 > x 12.5_B1
Material: Perforated plasterboard

Board Type: Gypsum panel

Dimensions: <900x2700x12.5mm> or <1200x2400x12.5mm>
	Weight: 9.20-9.90 kg/m²

Edge: B1
Perforation:  Square 12x12mm holes, c/c 30mm in patterns

Perforation percent: 7.8 - 13%

Surface: Unpainted cardboard

Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

65mm suspension with 50mm mineral wool (Q1F)

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.40 | 0.65 | 0.75 | 0.70 | 0.65 | 0.50 | 0.65 | 0.70 |

Installation

- c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.

- Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations.

- Mount the furring crosswise the primary construction at a max c/c on 300mm.

- Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide.

- Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.

- When filler is completely dry then sand with a fine sandpaper.

- Use a fine short-haired mohair roller to apply paint.

Acoustical deck and wall mount panels

Content

Screw fixed acoustic gypsum panel for ceiling and wall mount with 4 tapered edges for easy joint and filler.
Repaintable without loss of acoustics. 
100% recyclable product.

Products and materials

Tangent_900 x 2400 x 12.5_B1

Material: Perforated plasterboard

Board Type: Gypsum panel

Dimensions: 900 x 2400 x 12.5mm
	Weight: 9.20-9.90 kg/m²

Edge: B1
Perforation: Obround 4x14mm holes, c/c 10/20mm in patterns

Perforation percent: 13.3 - 15%

Surface: Unpainted cardboard
Fire rating: A2-s1,d0 in accordance with EN 13501-1
Indoor climate: Degasification 10 days
Particle emission: Low
Air purification: Cleaneo technology

Acoustics

65mm suspension with 50mm mineral wool (T3L1)

| 125 Hz | 250 Hz | 500 Hz | 1000 Hz | 2000 Hz | 4000 Hz | αw | NRC |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.35 | 0.60 | 0.70 | 0.70 | 0.65 | 0.65 | 0.70 | 0.65 |

Installation

- c/c distance for primary construction: max. 1000mm for wood and max. 1200mm for steel.

- Furring can be of wood (min. 60mm width) or steel (min. 45mm width) depending on current fire regulations.

- Mount the furring crosswise the primary construction at a max c/c on 300mm.

- Mount the acoustic gypsum panel crosswise on the furring and with a screw fixing distance c/c 300mm on the long edges and c/c 200mm on the short edges. Fixing distance inside the panel in depended on panel size and pattern and must be done in accordance with suppliers installation guide.

- Check that the screws have been countersunk and apply filler for both screws and edges in accordance with suppliers installation guide.

- When filler is completely dry then sand with a fine sandpaper.

- Use a fine short-haired mohair roller to apply paint.